|  |  |  |  |
| --- | --- | --- | --- |
| **Object no.** | **Date** | **Provenance of iron** | **Provenance of steel** |
| OBM4520 x1731 | 600-1050 CE | C1 (Western Jutland) | A1A (Norway and Northern Sweden) |
| OBM4937 x1399 | 750-1050 CE | C1 (Western Jutland) | A1A (Norway and Northern Sweden) |
| OBM8414 x278 | 750-1050 CE | B1 (possibly local) | A1A (Norway and Northern Sweden) |
| OBM8414 x339 | 750-1050 CE | C1 (Western Jutland) | A1B (Central- and Southern Sweden) |
| OBM8414 x378 | 750-1050 CE | A1B (Central- and Southern Sweden) | A1A (Norway and Northern Sweden) |
| OBM4520 x395 | 750-1050 CE | C1 (Western Jutland) | A3 (England) |
| OBM8414 x449 | 750-1050 CE | C1 (Western Jutland) | A2 (Germany and Central Europa) |
| OBM8414 x455 | 750-1050 CE | B1 (possibly local) | A1B (Central- and Southern Sweden) |
| OBM8414 x492 | 750-1050 CE | B1 (possibly local) | A1B (Central- and Southern Sweden) |
| OBM16224 x5 | 750-1050 CE | A1A (Norway and Northern Sweden) | A1A (Norway and Northern Sweden) |
| OBM4520 x1583 | 800-1000 CE | C1 (Western Jutland) | A1A (Norway and Northern Sweden) |
| OBM4520 x1634 | 800-1000 CE | C1 (Western Jutland) | A1A (Norway and Northern Sweden) |